NATURAL RESOURCES CONSERVATION SERVICE

CONSERVATION PRACTICE CONSTRUCTION SPECIFICATION

STREAMBANK AND SHORELINE PROTECTION - WIRE BOUND RIPRAP

CODE 580W

- SCOPE

The work shall consist of the construction of wire bound rock riprap including bedding.  This specification does not apply to gabions.

- SITE PREPARATION

Site preparation (mobilization and demobilization, clearing and grubbing, structure removal, pollution control, and water for construction) shall be in accordance with Construction Specification 587.

- MATERIALS

The wire mesh shall be galvanized steel wire (12 gage, minimum, with a Class 3 zinc coating), fabricated into double-twist mesh of non-raveling construction or welded wire mesh.  The mesh openings shall be uniform in size and shape.  Woven wire mesh shall be approximately 2½ inches by 3¼ inches in size and welded wire mesh shall be approximately 1½ inches by 3 inches in size, unless otherwise shown on the drawings.

Tie wire and lacing wire shall be 12-gage galvanized steel wire.

Rock shall be hard and durable and be approved by the engineer prior to placing.  The minimum rock size shall be 4 inches, the maximum rock size shall be 6 inches for a riprap thickness of 12 inches or less, and the maximum rock size shall be 9 inches for a riprap thickness greater than 12 inches.

Bedding shall be uniformly graded gravel ranging from ¼ inch to 2 inches.

Stakes shall be steel angles at least 2 x 2 x ¼ (inches) in dimension.

- FOUNDATION WORK

Foundation work (diverting surface water, dewatering the construction site, dewatering borrow areas, and foundation preparation) shall be in accordance with Construction Specification 587.

Bedding and/or riprap shall not be placed until the foundation preparation is completed and the subgrade surfaces have been inspected and approved by the engineer.

- EARTHWORK

Earthwork (common excavation and earthfill) shall be in accordance with Construction Specification 587.

- BEDDING

The bedding material shall be spread uniformly on the prepared foundation surface to the depth specified and shall be free of mounds, dips, or windrows.  Compacting of bedding will not be required.  The surface of the bedding shall be approved by the engineer prior to the placement of the rock riprap.

- PLACEMENT OF RIPRAP

The rock shall be placed on the surfaces and to the depths specified.  The riprap shall be constructed to the full course thickness in one operation and in such a manner as to avoid serious displacement of the underlying materials.  The rock shall be delivered and placed in a manner that will ensure that the riprap in place shall be reasonably homogeneous with the larger rocks uniformly disturbed and firmly in contact one to another with the smaller rocks and spalls filling the voids between the larger rocks.  Riprap shall be placed in a manner to prevent damage to structures.  Hand placing will be required to the extent necessary to prevent damage to the permanent works.

- PLACEMENT OF WIRE

The woven wire shall be placed on the bedding, then rock placed thereon, and the outer cage of wire placed over the rock.  The lower cage of wire shall be tied to the upper edge by interconnecting ties on a two-foot spacing grid pattern.  Woven wire shall overlap one-foot and spliced with ties on 6-inch spacings, except selvaged edges will not require overlap.  Use a loop with three full twists for all ties.  The finished job shall be a wire-bound riprap where the rock is fully enclosed by woven wire including the footing, ends, and sides.

Steel anchors shall be of the length as shown on the drawings and shall be driven into the riprap on five-foot centers in both directions.

- MEASUREMENT

The volume of the riprap and the volume of bedding will be separately measured within the specified limits as shown on the drawings and computed to the nearest cubic yard by the method of average cross-sectional end areas.

Project Name:

Date:

- ITEMS OF WORK AND CONSTRUCTION DETAILS

Items of work to be prepared in conformance with this specification and the construction details are: